Membrane

An Ultra Low Disturbance

Building Solution for damp walls and floors

Introduction

Kontract Trade Membrane is a plastic, dimpled sheet material for floor and wall applications.

It can be used to provide new interior wall and floor surfaces inside buildings, where the walls are old, salt contaminated or damp. Basements and cellars can be lined, with a sump pump fitted if necessary.

DESCRIPTION

Kontract Trade Membrane is a plastic, dimpled sheet supplied on a 2 metre wide roll 20 metres in length. The surface can be directly fitted with plasterboard or dry lined on battens, (for walls), or screeded or fitted with a ‘floating’ floor (chipboard, 22mm) on floors.

TECHNICAL DATA

Material

Studded Polyethylene, 7.5mm thick, made from 0.5mm, 2500 gauge plastic

Other Components

Plastic plugs, seals, tape for joints, corner tape

Size

Roll 2 metres wide, 20 metres long giving an effective area of cover of 36 square metres (after deducting overlaps)

Fixing size - wall plugs

Black plugs 11mm diameter x 73mm long, with holes in the heads for No.12 s/t screws, hole depth 30mm plus add batten thickness.

Hole size for drilling - wall plugs

Drill 10mm diameter holes, 76mm long

Fixing spacing - wall plugs

At 600mm centres vertically x plasterboard width = average 4 plugs per square metre

PROPERTY REPAIR SYSTEMS

Tel: 01626 331351 Fax: 01626 331143

Special features

·	Easy fix hammer in plugs for wall lining

·	Easy lay on the floor, no fixings, with taped joints

·	Plug seals and joint tape included

·	Guaranteed

TRADE KIT

BBA Cert. No:05/4261

USES

To provide new, dry decorative surfaces in old buildings where the walls or floors have been contaminated with ‘salts’ or dampness, or are partially below ground level, but only where no liquid water is present. (It can also be used as part of full cellar or basement conversions, with the addition of a sump pump.)

PREPARATION & APPLICATION

Walls only - Hack off all plaster and contaminated render to bare brick or stone. Brush off all loose material. Check the roll size compared to the wall areas to be covered, allowing for an overlap between sheets of 100mm. Keep all materials dust free during cutting and fixing. Prepare the plugs by fitting a rubber seal washer to each plug head, to seal against water vapour ingress. Drill 10mm holes about 76mm deep. Hammer the fixing plugs through the membrane until the seals are squeezed against the sheet surface. When butting sheets together apply the black, butyl tape to the overlap and press surfaces firmly together. Allow an air gap top and bottom. Fix battens with self tapping screws and align with wedges. Attach plasterboard & skim finish.

Floors - install sub floor drainage, if liquid water is ever present. Lay dimple side down. Tape the joints. Use Corner Tape at floor to wall junction. Lay insulation (optional) under treated chipboard or, for uneven floors apply a 50mm sand/cement screed.